## Slide 1
FE Model
Compare the GO-PVA experiment with simulation result
Pile ups of GO based PVA films by the indentation
Substrate which consist of GO and PVA has 35 stacks.
We used berkovich tip and experiment was conducted in three steps. In first step, the load steadily increased to 200 μN for 5 seconds. In second step, the load maintained for 5 seconds. In last step, the load removed steadily for 5 seconds.
On this research, we used ABAQUS(FEM commercial software, ABAQUS Inc.,USA) to simulate the Nano-Indentation experiment.
Viscoelastic material could be defined by using Prony series expansion of the dimensionless relaxation modulus in ABAQUS. In Prony series, there are 3 parameters() to define the viscoelastic material.
Boundary Condition | Material Property | Load
Hyeonho Cho1,†, JoonHo Lee2,†, jin-Gyun Kim2,*, Sunghan Kim1,*
1 School of Mechanical Engineering, Chung-Ang University, Seoul, Republic of Korea
2 Department of Mechanical Engineering, Kyung Hee University, Yongin, Republic of Korea
† Author Contributions: H. Cho and J. Lee contributed equally to this work. * Correspondence: jingyun.kim@khu.ac.kr; sunghankim@cau.ac.kr
Mechanical Properties of GO Based Thin Polymer Films: Experiment and Simulation
Introduction
Material & Method
Discuss
Conclusion
Chart: depth(nm)
We used the berkovich tip model as a rigid body because we assumed that there is no deformation on tip.
Young’s modulus and Possion’s ratio of material that make up the composite have a large range of value. So, we used general value of material property.
 | E (Gpa) | nu
GO | 150 | 0.3
PVA | 5 | 0.45
Chart: Time (sec)
concentrated force
B.C | Substrate | Tip
U1 | V | V
U2 | V | V
U3 | V | -
UR1 | V | V
UR2 | V | V
UR3 | V | V
GO
PVA
. . .
GO
PVA
1 stack
( 7 nm )
35 stacks
( 245 nm )
1 nm
6 nm
1 nm
6 nm
Result
Various methods are used for fabricating thin polymer films. Among them, the thin polymer films, which are synthesized by LbL method, can be used to provide enhancing mechanical robustness for certain engineering products.
Even though many studies are actively pursued for improving the durability of GO-based LbL films, there is a lack of fundamental knowledge about their mechanical properties.
This present research examines both the hardness and the elastic modulus of graphene GO-based thin polymer films by using Nano-Indentation experiments.
We used FEM method on this research to Verify results of Nano-Indentation experiments.
0.1494 | 0 | 0.4500
0.2940 | 0 | 0.4500
0.1045 | 0 | 0.3400
0.0700 | 0 | 0.3300
0.0600 | 0 | 0.6896
0.0400 | 0 | 6.7010
0.0800 | 0 | 100.0000
0.0710 | 0 | 1600.0000
0.0750 | 0 | 12400.0000
0.1494 | 0 | 0.4500
0.2940 | 0 | 0.4500
0.1045 | 0 | 0.3400
0.0700 | 0 | 0.3300
0.0600 | 0 | 0.6896
0.0400 | 0 | 6.7010
0.0800 | 0 | 100.0000
0.0710 | 0 | 1600.0000
0.0750 | 0 | 12400.0000
Elastic
Viscoelastic
z
x
y
GO-based thin polymer films were fabricated by LbL self-assembly technique.
The mechanical properties, such as the elastic modulus and the hardness of GO based PVA films, were investigated by nanoindentation and FEM analysis. It is found that the mechanical properties of the film structures are mainly affected by interfacial bonding strength.
Figure 1. a) TriboScope nanoindentation device (TS 75Hysitron, Inc.), b) Schematic diagram of a typical load displacement curve during an indentation experiment, c) Schematic diagram of a typical indented surface during indentaion experiment.
Experimental Details
P: applied load, E: elastic modulus, M: indentaion modulus, H: hardness, A: contact area, h: indentation depth, v: poisson’s ratio
(1) Vadukumpully, S.; Paul, J.; Mahanta, N.; Valiyaveettil, S., 2011, “Flexible conductive graphene/poly (vinyl chloride) composite thin films with high mechanical strength and thermal stability.”, Carbon, Vol. 49, No.1, pp.198.
(2) Luong, N. D.; Hippi, U.; Korhonen, J. T.; Soininen, A. J.; Ruokolainen, J.; Johansson, L.-S.; Nam, J.-D.; Seppälä, J., 2011, “Enhanced mechanical and electrical properties of polyimide film by graphene sheets via in situ polymerization.”, Polymer, Vol.52, No.23, pp.5237.
(3) Kim, S.; Xiong, R.; Tsukruk, V. V., 2016 “Probing Flexural Properties of Cellulose Nanocrystal–Graphene Nanomembranes with Force Spectroscopy and Bulging Test.”, Langmuir, Vol. 32, No. 21, pp.5383.
(4) Das, B.; Prasad, K. E.; Ramamurty, U.; Rao, C., 2009, “Nano-indentation studies on polymer matrix composites reinforced by few-layer graphene.” Nanotechnology, Vol. 20, No. 12, pp.125705.
Figure 2. Image of indented surface of reduced GO based PVA films on Si substrate after a) low load indentation experiment under 110 uN and b) high load indentation experiment under 2mN load.
The contact area between the tip and the target surface can be significantly increased due to the pile ups.
5th International Conference on Materials and Reliability, November 27-29, 2019, Maison Glad Jeju, Jeju, Korea